## Slide 1
PdO Sobol
#14 shows carrier concentration of 1.74E+19/cm3 and mobility of 9.91cm2/V·s.
Due to the low oxidation time (1.1min,) the variance between run is very high.
Transistors will be made with these parameters.
Is it possible to base future parameters on #14?
My instinct that I cannot guarantee to be correct is dep pressure is more important than dep O2 flow rate, high dep temp is better, low ox pressure is better.
Replicate | Dep Power (W) | O2 Flow (sccm) | Dep Press (mTorr) | Dep Temp (°C) | Ox Temp (°C) | Ox Press (atm) | Ox Time (min) | Vac Ann Temp (°C) | Vac Ann Time (min) | Dep Thickness (nm) | Hall mobility (cm^2/V*s) | Carrier concentration (#/cm^3)
1 | 36 | 13.4 | 6.3 | 425 | 694.7 | 0.02 | 1.1 | 217.4 | 29.1 | 7.8 | 9.91 | 1.74E+19
2 | 36 | 13.4 | 6.3 | 425 | 694.7 | 0.02 | 1.1 | 217.4 | 29.1 | 7.8 | <Contact Fail> | <Contact Fail>
3 | 36 | 13.4 | 6.3 | 425 | 694.7 | 0.02 | 1.1 | 217.4 | 29.1 | 7.8 | 6.28 | 1.53E+19

## Slide 2
PdO Sobol
All 23 experimental splits are finished.
Thickness of annealed film is estimated base on previous XRR values (3nm as deposited film grew into 5nm film after oxidation.)
Vacuum anneal at higher than ~550℃ cause contact fail, possibly due to discontinuous film.
#11 shows contact fail but vacuum anneal temperature is <500℃.
#17 shows contact fail due to no deposition.
Low oxidation pressure seems to be important. I’ll try reducing oxygen flow rate to see if we can get lower pressure without hampering oxidation.
Base_Run_ID | Replicate | Dep Power (W) | O2 Flow (sccm) | Dep Press (mTorr) | Dep Temp (°C) | Ox Temp (°C) | Ox Press (atm) | Ox Time (min) | Vac Ann Temp (°C) | Vac Ann Time (min) | Dep Thickness (nm) | Batch | Dep Rate (nm/min) | Dep Time (min) | min | sec | Hall mobility (cm^2/V*s) | Carrier concentration (#/cm^3)
1 | 1 | 3 | 4.4 | 4.3 | 425 | 557 | 1 | 98.8 | 584.1 | 90.1 | 7.7 | Batch 1 | 0.24 | 32.08333 | 32 | 5 | <Contact Fail> | <Contact Fail>
1 | 2 | 3 | 4.4 | 4.3 | 425 | 557 | 1 | 98.8 | 584.1 | 90.1 | 7.7 | Batch 1 | 0.24 | 32.08333 | 32 | 5 | <Contact Fail> | <Contact Fail>
1 | 3 | 3 | 4.4 | 4.3 | 425 | 557 | 1 | 98.8 | 584.1 | 90.1 | 7.7 | Batch 1 | 0.24 | 32.08333 | 32 | 5 | <Contact Fail> | <Contact Fail>
2 | 1 | 28 | 11.5 | 9.7 | 25 | 476.8 | 0.02 | 14.3 | 155.4 | 18.1 | 5.1 | Batch 1 | 1.6 | 3.1875 | 3 | 11 | 4.36 | 1.74E+20
2 | 2 | 28 | 11.5 | 9.7 | 25 | 476.8 | 0.02 | 14.3 | 155.4 | 18.1 | 5.1 | Batch 1 | 1.6 | 3.1875 | 3 | 11 | 4.33 | 1.60E+20
2 | 3 | 28 | 11.5 | 9.7 | 25 | 476.8 | 0.02 | 14.3 | 155.4 | 18.1 | 5.1 | Batch 1 | 1.6 | 3.1875 | 3 | 11 | 4.49 | 1.58E+20
3 | 1 | 40 | 9.1 | 3.4 | 425 | 262.5 | 0.02 | 71.7 | 400 | 57.9 | 2.2 | Batch 1 | 4.8 | 0.458333 | 0 | 28 | 3.89 | 1.96E+20
3 | 2 | 40 | 9.1 | 3.4 | 425 | 262.5 | 0.02 | 71.7 | 400 | 57.9 | 2.2 | Batch 1 | 4.8 | 0.458333 | 0 | 28 | 4.14 | 1.92E+20
3 | 3 | 40 | 9.1 | 3.4 | 425 | 262.5 | 0.02 | 71.7 | 400 | 57.9 | 2.2 | Batch 1 | 4.8 | 0.458333 | 0 | 28 | 4.26 | 1.83E+20
4 | 1 | 14 | 16.9 | 6.6 | 25 | 774.1 | 1 | 39.9 | 728.4 | 73.6 | 9.3 | Batch 1 | 1 | 9.3 | 9 | 18 | <Contact Fail> | <Contact Fail>
4 | 2 | 14 | 16.9 | 6.6 | 25 | 774.1 | 1 | 39.9 | 728.4 | 73.6 | 9.3 | Batch 1 | 1 | 9.3 | 9 | 18 | <Contact Fail> | <Contact Fail>
4 | 3 | 14 | 16.9 | 6.6 | 25 | 774.1 | 1 | 39.9 | 728.4 | 73.6 | 9.3 | Batch 1 | 1 | 9.3 | 9 | 18 | <Contact Fail> | <Contact Fail>
5 | 1 | 19 | 7 | 8.5 | 25 | 661.6 | 1 | 82.5 | 288.6 | 31 | 3.5 | Batch 1 | 1.4 | 2.5 | 2 | 30 | 1.91 | 5.61E+19
5 | 2 | 19 | 7 | 8.5 | 25 | 661.6 | 1 | 82.5 | 288.6 | 31 | 3.5 | Batch 1 | 1.4 | 2.5 | 2 | 30 | 2.62 | 4.60E+19
5 | 3 | 19 | 7 | 8.5 | 25 | 661.6 | 1 | 82.5 | 288.6 | 31 | 3.5 | Batch 1 | 1.4 | 2.5 | 2 | 30 | 2.06 | 5.29E+19
6 | 1 | 34 | 19.1 | 5.6 | 425 | 300 | 0.02 | 58.2 | 620.4 | 77.2 | 5.9 | Batch 1 | 3.1 | 1.903226 | 1 | 54 | <Contact Fail> | <Contact Fail>
6 | 2 | 34 | 19.1 | 5.6 | 425 | 300 | 0.02 | 58.2 | 620.4 | 77.2 | 5.9 | Batch 1 | 3.1 | 1.903226 | 1 | 54 | <Contact Fail> | <Contact Fail>
6 | 3 | 34 | 19.1 | 5.6 | 425 | 300 | 0.02 | 58.2 | 620.4 | 77.2 | 5.9 | Batch 1 | 3.1 | 1.903226 | 1 | 54 | <Contact Fail> | <Contact Fail>
7 | 1 | 23 | 1.6 | 7.3 | 25 | 364.3 | 0.02 | 118 | 474.1 | 117 | 8.6 | Batch 1 | 2.2 | 3.909091 | 3 | 55 | 7.25 | 5.66E+19
7 | 2 | 23 | 1.6 | 7.3 | 25 | 364.3 | 0.02 | 118 | 474.1 | 117 | 8.6 | Batch 1 | 2.2 | 3.909091 | 3 | 55 | 6.71 | 5.85E+19
7 | 3 | 23 | 1.6 | 7.3 | 25 | 364.3 | 0.02 | 118 | 474.1 | 117 | 8.6 | Batch 1 | 2.2 | 3.909091 | 3 | 55 | 6.58 | 5.81E+19
8 | 1 | 8 | 14.2 | 2.6 | 425 | 594.5 | 1 | 26.1 | 48.9 | 14.6 | 1.7 | Batch 1 | 0.8 | 2.125 | 2 | 8 | 1.70 | 1.19E+20
8 | 2 | 8 | 14.2 | 2.6 | 425 | 594.5 | 1 | 26.1 | 48.9 | 14.6 | 1.7 | Batch 1 | 0.8 | 2.125 | 2 | 8 | 1.43 | 1.47E+20
8 | 3 | 8 | 14.2 | 2.6 | 425 | 594.5 | 1 | 26.1 | 48.9 | 14.6 | 1.7 | Batch 1 | 0.8 | 2.125 | 2 | 8 | 1.34 | 1.85E+20
9 | 1 | 7 | 8.7 | 7.6 | 425 | 429.6 | 1 | 81 | 229.6 | 42.4 | 9.6 | Batch 1 | 0.48 | 20 | 20 | 0 | 2.98 | 5.51E+19
9 | 2 | 7 | 8.7 | 7.6 | 425 | 429.6 | 1 | 81 | 229.6 | 42.4 | 9.6 | Batch 1 | 0.48 | 20 | 20 | 0 | 3.14 | 4.55E+19
9 | 3 | 7 | 8.7 | 7.6 | 425 | 429.6 | 1 | 81 | 229.6 | 42.4 | 9.6 | Batch 1 | 0.48 | 20 | 20 | 0 | 2.84 | 5.06E+19
10 | 1 | 22 | 15.7 | 2.4 | 25 | 536.8 | 0.02 | 45.4 | 655.2 | 88.1 | 3 | Batch 1 | 2.5 | 1.2 | 1 | 12 | <Contact Fail> | <Contact Fail>
10 | 2 | 22 | 15.7 | 2.4 | 25 | 536.8 | 0.02 | 45.4 | 655.2 | 88.1 | 3 | Batch 1 | 2.5 | 1.2 | 1 | 12 | <Contact Fail> | <Contact Fail>
10 | 3 | 22 | 15.7 | 2.4 | 25 | 536.8 | 0.02 | 45.4 | 655.2 | 88.1 | 3 | Batch 1 | 2.5 | 1.2 | 1 | 12 | <Contact Fail> | <Contact Fail>
11 | 1 | 31 | 3.7 | 8.7 | 425 | 732.2 | 0.02 | 108.5 | 415.1 | 105.6 | 4.7 | Batch 1 | 2.6 | 1.807692 | 1 | 48 | <Contact Fail> | <Contact Fail>
11 | 2 | 31 | 3.7 | 8.7 | 425 | 732.2 | 0.02 | 108.5 | 415.1 | 105.6 | 4.7 | Batch 1 | 2.6 | 1.807692 | 1 | 48 | <Contact Fail> | <Contact Fail>
11 | 3 | 31 | 3.7 | 8.7 | 425 | 732.2 | 0.02 | 108.5 | 415.1 | 105.6 | 4.7 | Batch 1 | 2.6 | 1.807692 | 1 | 48 | <Contact Fail> | <Contact Fail>
12 | 1 | 15 | 11.3 | 5.3 | 25 | 231.1 | 1 | 20.3 | 83.7 | 3.6 | 6.9 | Batch 1 | 1.4 | 4.928571 | 4 | 56 | 0.94 | 2.79E+20
12 | 2 | 15 | 11.3 | 5.3 | 25 | 231.1 | 1 | 20.3 | 83.7 | 3.6 | 6.9 | Batch 1 | 1.4 | 4.928571 | 4 | 56 | 0.90 | 2.68E+20
12 | 3 | 15 | 11.3 | 5.3 | 25 | 231.1 | 1 | 20.3 | 83.7 | 3.6 | 6.9 | Batch 1 | 1.4 | 4.928571 | 4 | 56 | 0.67 | 3.24E+20
13 | 1 | 10 | 1.5 | 3.7 | 25 | 343.6 | 1 | 96.8 | 546.2 | 101.5 | 1.5 | Batch 1 | 1.2 | 1.25 | 1 | 15 | <Contact Fail> | <Contact Fail>
13 | 2 | 10 | 1.5 | 3.7 | 25 | 343.6 | 1 | 96.8 | 546.2 | 101.5 | 1.5 | Batch 1 | 1.2 | 1.25 | 1 | 15 | <Contact Fail> | <Contact Fail>
13 | 3 | 10 | 1.5 | 3.7 | 25 | 343.6 | 1 | 96.8 | 546.2 | 101.5 | 1.5 | Batch 1 | 1.2 | 1.25 | 1 | 15 | <Contact Fail> | <Contact Fail>
14 | 1 | 36 | 13.4 | 6.3 | 425 | 694.7 | 0.02 | 1.1 | 217.4 | 29.1 | 7.8 | Batch 1 | 3.1 | 2.516129 | 2 | 31 | 9.91 | 1.74E+19
14 | 2 | 36 | 13.4 | 6.3 | 425 | 694.7 | 0.02 | 1.1 | 217.4 | 29.1 | 7.8 | Batch 1 | 3.1 | 2.516129 | 2 | 31 | <Contact Fail> | <Contact Fail>
14 | 3 | 36 | 13.4 | 6.3 | 425 | 694.7 | 0.02 | 1.1 | 217.4 | 29.1 | 7.8 | Batch 1 | 3.1 | 2.516129 | 2 | 31 | 6.28 | 1.53E+19
15 | 1 | 27 | 6 | 4.5 | 25 | 649.3 | 0.02 | 62.7 | 362.2 | 46.5 | 6.2 | Batch 1 | 3 | 2.066667 | 2 | 4 | 8.68 | 3.16E+19
15 | 2 | 27 | 6 | 4.5 | 25 | 649.3 | 0.02 | 62.7 | 362.2 | 46.5 | 6.2 | Batch 1 | 3 | 2.066667 | 2 | 4 | 8.91 | 3.17E+19
15 | 3 | 27 | 6 | 4.5 | 25 | 649.3 | 0.02 | 62.7 | 362.2 | 46.5 | 6.2 | Batch 1 | 3 | 2.066667 | 2 | 4 | 8.94 | 3.26E+19
16 | 1 | 2 | 18.5 | 9.5 | 425 | 392.1 | 1 | 34.7 | 790.5 | 62.7 | 4.4 | Batch 1 | 0.06 | 73.33333 | 73 | 20 | <Contact Fail> | <Contact Fail>
16 | 2 | 2 | 18.5 | 9.5 | 425 | 392.1 | 1 | 34.7 | 790.5 | 62.7 | 4.4 | Batch 1 | 0.06 | 73.33333 | 73 | 20 | <Contact Fail> | <Contact Fail>
16 | 3 | 2 | 18.5 | 9.5 | 425 | 392.1 | 1 | 34.7 | 790.5 | 62.7 | 4.4 | Batch 1 | 0.06 | 73.33333 | 73 | 20 | <Contact Fail> | <Contact Fail>
17 | 1 | 0 | 5.4 | 2.1 | 25 | 790.9 | 0.02 | 10.8 | 322.7 | 85.6 | 5.7 | Batch 1 | 0 | #DIV/0! | #DIV/0! | #DIV/0! | <Contact Fail> | <Contact Fail>
17 | 2 | 0 | 5.4 | 2.1 | 25 | 790.9 | 0.02 | 10.8 | 322.7 | 85.6 | 5.7 | Batch 1 | 0 | #DIV/0! | #DIV/0! | #DIV/0! | <Contact Fail> | <Contact Fail>
17 | 3 | 0 | 5.4 | 2.1 | 25 | 790.9 | 0.02 | 10.8 | 322.7 | 85.6 | 5.7 | Batch 1 | 0 | #DIV/0! | #DIV/0! | #DIV/0! | <Contact Fail> | <Contact Fail>
18 | 1 | 26 | 17.9 | 7.9 | 425 | 243 | 1 | 102.5 | 757.3 | 37.6 | 3.5 | Batch 1 | 1.8 | 1.944444 | 1 | 57 | <Contact Fail> | <Contact Fail>
18 | 2 | 26 | 17.9 | 7.9 | 425 | 243 | 1 | 102.5 | 757.3 | 37.6 | 3.5 | Batch 1 | 1.8 | 1.944444 | 1 | 57 | <Contact Fail> | <Contact Fail>
18 | 3 | 26 | 17.9 | 7.9 | 425 | 243 | 1 | 102.5 | 757.3 | 37.6 | 3.5 | Batch 1 | 1.8 | 1.944444 | 1 | 57 | <Contact Fail> | <Contact Fail>
19 | 1 | 37 | 0.8 | 5.2 | 25 | 497.4 | 1 | 43.8 | 512.8 | 6.1 | 1.9 | Batch 1 | 4.3 | 0.44186 | 0 | 27 | 2.28 | 2.36E+20
19 | 2 | 37 | 0.8 | 5.2 | 25 | 497.4 | 1 | 43.8 | 512.8 | 6.1 | 1.9 | Batch 1 | 4.3 | 0.44186 | 0 | 27 | 2.49 | 2.01E+20
19 | 3 | 37 | 0.8 | 5.2 | 25 | 497.4 | 1 | 43.8 | 512.8 | 6.1 | 1.9 | Batch 1 | 4.3 | 0.44186 | 0 | 27 | 2.47 | 2.12E+20
20 | 1 | 12 | 12.8 | 8.8 | 425 | 539 | 0.02 | 68.2 | 178.3 | 110.4 | 8.6 | Batch 1 | 0.7 | 12.28571 | 12 | 17 | 7.28 | 2.50E+19
20 | 2 | 12 | 12.8 | 8.8 | 425 | 539 | 0.02 | 68.2 | 178.3 | 110.4 | 8.6 | Batch 1 | 0.7 | 12.28571 | 12 | 17 | 7.66 | 2.74E+19
20 | 3 | 12 | 12.8 | 8.8 | 425 | 539 | 0.02 | 68.2 | 178.3 | 110.4 | 8.6 | Batch 1 | 0.7 | 12.28571 | 12 | 17 | 7.67 | 2.59E+19
21 | 1 | 17 | 3.1 | 6.1 | 425 | 576.5 | 0.02 | 54.5 | 454.7 | 24.7 | 5.4 | Batch 1 | 1.7 | 3.176471 | 3 | 11 | 7.48 | 5.16E+19
21 | 2 | 17 | 3.1 | 6.1 | 425 | 576.5 | 0.02 | 54.5 | 454.7 | 24.7 | 5.4 | Batch 1 | 1.7 | 3.176471 | 3 | 11 | 7.37 | 4.56E+19
21 | 3 | 17 | 3.1 | 6.1 | 425 | 576.5 | 0.02 | 54.5 | 454.7 | 24.7 | 5.4 | Batch 1 | 1.7 | 3.176471 | 3 | 11 | 7.67 | 4.95E+19
22 | 1 | 32 | 10.7 | 3.9 | 25 | 384.9 | 1 | 86.4 | 116.8 | 98.5 | 7.2 | Batch 1 | 3.6 | 2 | 2 | 0 | 5.58 | 1.28E+20
22 | 2 | 32 | 10.7 | 3.9 | 25 | 384.9 | 1 | 86.4 | 116.8 | 98.5 | 7.2 | Batch 1 | 3.6 | 2 | 2 | 0 | 4.98 | 1.38E+20
22 | 3 | 32 | 10.7 | 3.9 | 25 | 384.9 | 1 | 86.4 | 116.8 | 98.5 | 7.2 | Batch 1 | 3.6 | 2 | 2 | 0 | 4.89 | 1.38E+20
23 | 1 | 21 | 8.1 | 9.1 | 425 | 280.5 | 1 | 30 | 263.1 | 67.1 | 9 | Batch 1 | 1.5 | 6 | 6 | 0 | 0.92 | 5.01E+19
23 | 2 | 21 | 8.1 | 9.1 | 425 | 280.5 | 1 | 30 | 263.1 | 67.1 | 9 | Batch 1 | 1.5 | 6 | 6 | 0 | 1.01 | 3.87E+19
23 | 3 | 21 | 8.1 | 9.1 | 425 | 280.5 | 1 | 30 | 263.1 | 67.1 | 9 | Batch 1 | 1.5 | 6 | 6 | 0 | 1.01 | 3.34E+19

## Slide 3
PdO Sobol
Dep Power (W) | O2 Flow (sccm) | Dep Press (mTorr) | Dep Temp (°C) | Ox Temp (°C) | Ox Press (atm) | Ox Time (min) | Vac Ann Temp (°C) | Vac Ann Time (min) | Dep Thickness (nm)
Hall mobility (cm^2/V*s) | Carrier concentration (#/cm^3)
Since every parameter can be finetuned individually, and every parameter changes mobility as well as concentration, the graph should look like this. Mobility and carrier concentration also influence each other.